## Slide 1: Coupling direct numerical simulation with population balance modelling for predicting turbulent particle precipitation in a T-mixer
Hin Yan TANG1, George PAPADAKIS2, Stelios RIGOPOULOS1
1 Department of Mechanical Engineering, Imperial College London, UK
2 Department of Aeronautics, Imperial College London, UK

## Slide 2: What is particle precipitation?
Mixing reactants
Supersaturated Solution
Reaction between chemical species
Phase change
  -A process that forms particulate product
Nucleation
Growth
Aggregation
Breakage
L.Metzger, et.al (2016)
The product quality usually correlates with the particle size distribution (PSD)

## Slide 3: Challenges
Precipitation is highly sensitive to the local composition
  Fast changing kinetics
Fast reaction-precipitation
  Small precipitation time scale
PSD is changing rapidly in space and in time
Local information can hardly be captured by experiments
Motivation
Numerical simulations open a door to understand the physics in turbulent precipitation
Develop a coupled DNS-PBE approach for simulating particulate process in turbulent flow

## Slide 4: Coupling between DNS and Population Balance Modelling

## Slide 5: Direct numerical simulation (DNS)
N-S equations:
Transport for ions:
Fraction step
BDF3 for time advancement
Implicit diffusion and explicit convection

## Slide 6: Population Balance Modelling
Particle number
  Discretised into intervals
  Number density
  General form of Population Balance Equation (PBE) for particulate processes
Evolution of Number density distribution in time
Transient term
Generation term due to aggregation
Destruction term due to aggregation
N Total number of particles
Number density
L Size interval (Class)
B0 Nucleation term
B Generation term
D Destruction term
G Growth rate
L L+dL
:number of
at t
at t+dt
Growth term
Nucleation term
Generation term due to breakage
Destruction term due to breakage
S. Rigopoulos (2010)

## Slide 7
The flow field is captured by DNS, which can be considered as fully resolved
The only modelling terms are the growth and nucleation rates
These kinetics depends on the supersaturation (driving force) and are non-linear
Semi-empirical relations
Source term
Nucleation
Growth
Number transport
Assume particles as tracer
PBE is solved locally in each cell together with the DNS
The PBE source terms are used also in the computation of ion consumption to achieve coupling with ion transport
Convection term
Diffusion term

## Slide 8: Discretisation on the Particle Size Distribution (PSD)
Particle size range is discretised into 45 intervals ( j = 1 - 45 ) with a composite grid

## Slide 9: Nanoparticle precipitation in a T-mixer
Apply the coupled DNS-PBE approach to the nano-particle precipitation of BaSO4 in a T-mixer (H.-C. Schwarzer, 2004)
What are the effects of mixing on the precipitation process ?
How the PSD is influenced by local effects ?
0.5M BaCl2
0.33M H2SO4
H.-C. Schwarzer, et. Al (2004)
3D Cartesian mesh
21 million cells
Flow field is fully resolved to Kolmogorov scale

## Slide 10: The kinetics
Supersaturation
Precipitation timescales
Nucleation rate
Growth rate
Homogeneous nucleation and transport-controlled growth is employed as suggested by Gradl & Peukert (2009) and is taken from the classical theory. (Mersmann, 2000)

## Slide 11: Flow field & Mixing
Re = 1135
,Turbulent at Re>400 (Telib et al., 2004)
Helical Pattern
Intense mixing at impingement zone
Fastest mixing time scale in the order of 10-5
Micro-mixing (Engulfment) time scale
(characterizes the timescale of the most energetic vortex)
Streamline

## Slide 12: The PSD
A
B
C
A
D
E
F
G
H
0.5M BaCl2
0.33M H2SO4

## Slide 13: The local kinetics
Supersaturation
Growth timescale
Nucleation timescale
0.5M BaCl2
0.33M H2SO4

## Slide 14: Intermittency
Non-linear kinetics and turbulent mixing leads to highly intermittent formation.

## Slide 15: Conditional timescales

## Slide 16: Damköhler numbers
Nucleation and growth have their own timescales.
Two Damköhler numbers can be defined:

## Slide 17: Local dominance zone and its mapping with supersaturation
Growth
dominance
zone
Competing
zone
Nucleation
dominance
zone
High correspondence to the supersaturation map
Nucleation dominance: S > 700
Competing: 400 < S < 800
Growth dominance: S < 550

## Slide 18: Characteristics of each dominance zone
Growth
dominance
zone
Competing
zone
Nucleation
dominance
zone
The PSD in each zone exhibits different characteristics.
The area / volume distribution of each zone has determining effects on the final PSD.
How area / volume of these zone changes with Reynolds number is currently under investigation.

## Slide 19
Mean plane averaged PSD

## Slide 20: Conclusions
DNS – PBE coupled approach is developed an is applied on BaSO4 precipitation
Excellent agreement with measurement
Different dominance zone and their contribution can be identified

## Slide 21: Thank you

## Slide 22: Moment of distribution
Supersaturation
0th Moment
(No. of particle per unit volume)
1st Moment
(Crystal volume per unit volume)

## Slide 23
Intensity of Segregation
(a measure of evenness)

## Slide 24: Intensity of segregation
A measure of evenness
1 - Fully segregated
0 – Homogeneously mixed

## Slide 25: Flow field obtained from DNS
t=10 s
t=140 s
t=150 s
t=180 s

## Slide 26: Flow field obtained from DNS (cont’d)
x
y
z
x/H=0
x/H=0.25
x/H=0.75
x/H=2.75
H

## Slide 27: Compare with experimental PIV results[4]
x/H = 0
[4] F. Schwertfirm, J. Gradl, H. Schwarzer, W. Peukert and M. Manhart, “The low Reynolds number turbulent flow and mixing in a confined impinging jet reactor,” International Journal of Heat and Fluid Flow, vol. 28, pp. 1429-1442, 2007.
x/H = 0.25
x/H = 2.75
x/H = 0.75

## Slide 28: Velocity Profile (preliminary comparison with experimental results[4] )
[4] F. Schwertfirm, J. Gradl, H. Schwarzer, W. Peukert and M. Manhart, “The low Reynolds number turbulent flow and mixing in a confined impinging jet reactor,” International Journal of Heat and Fluid Flow, vol. 28, pp. 1429-1442, 2007.